## Slide 1: AI-driven image segmentation for accurate characterization of wettability
Yang Gao
Co author: Sajjad Foroughi, Jack Ma
Supervisor: Martin Blunt, Branko Bijeljic
Pore-Scale Modelling and Imaging

## Slide 2: Now it's 2024! Volumetric neural networks?
Computationally demanding
We spend many times the computational resources than normal methods. It does not result in significant gains in accuracy
Many parameters and difficult to train
The number of network parameters is huge and requires a lot of data for training. But so far these have not appeared to be better generalizable (trained with one sample, applied on other samples).
5 times computational resources for 1% improvement
Ying Da Wang, Mehdi Shabaninejad, Ryan T. Armstrong, Peyman Mostaghimi. Deep neural networks for improving physical accuracy of 2D and 3D multi-mineral segmentation of rock micro-CT images, 2021. Applied Soft Computing,Volume 104,2021,107185, ISSN 1568-4946

## Slide 3: GGIECN
Grey-scale gradient information enhanced convolutional network
Automatic correction for manual bias
Generalizability for various wettability
Generalizability for various lithology
Low computational requirements
High-precision interface segmentation

## Slide 4: GGIECN & Automatic CA Measurement Workflow
Convey 3D structural information and segment effectively with limited graphics memory by processing images in XY and XZ directions separately
Only 40% of the data was used as training data, plus automatically extracted gradient information. We obtained wettability evaluation results that are more consistent with the physical mechanism than the training dataset.

## Slide 5: Canny – An objective method to identify boundaries based on grey-scale gradients
X direction gradient information Gx is calculated as:
Y direction gradient information Gy is calculated as:
The gradient magnitude G is calculated as:
The azimuthal angle θ is calculated as:
Gradient boundaries are identified perpendicular to θ.

## Slide 6: Comprehensive loss function
Basic image segmentation loss
Gradient boundary and training dataset boundary loss
Additional phase segmentation penalty for the disputed voxels on the predicted boundary

## Slide 7: Gradient boundaries – Ketton Limestone

## Slide 8: Water-wet Ketton limestone
40% of the result from watershed was used as the training dataset.
The voxel accuracy of the validation set is around 98%.
Fluid surfaces are more reasonable.
This helps to improve contact angle measurement.
Image
GGIECN
Watershed

## Slide 9: Water-wet Ketton limestone
Yang, J., & Zhou, Y. (2020). An automatic in situ contact angle determaination based on level set method. Water Resources Research, 56 (7),479
Both the segmentation method and the contact angle measurement method are different with Jianhui Yang, While the measured results are basically the same.

## Slide 10: Gradient boundaries - Bentheimer sandstone

## Slide 11: Water-wet Bentheimer sandstone
40% of the result from watershed was used as the training dataset.
The voxel accuracy of the validation set is around 96%.
Eliminates meaningless three-phase contact points due to low resolution
Image
GGIECN
Watershed

## Slide 12
Mixed-wet Bentheimer sandstone
Image
GGIECN
Watershed
40% of the result from watershed was used as the training dataset.
The voxel accuracy of the validation set is around 96%.
Effectively filters out the abnormal segmentation contained in training dataset.

## Slide 13
Water-wet & Mixed-wet Bentheimer sandstone
Lin, Q., Bijeljic, B., Berg, S., Pini, R., Blunt, M. J., & Krevor, S. (2019, Jun). Minimal surfaces in porous media: Pore-scale imaging of multiphase flow in an altered-wettability bentheimer sandstone. Phys. Rev. E, 99 , 063105.
There are fewer contact points in GGIECN as it effectively filters out the abnormal points with the help of gradient information.

## Slide 14: Gradient boundaries - reservoir carbonate

## Slide 15
Water-wet reservoir carbonate
Image
GGIECN
WEKA
Verify the applicability of the workflow under complex structural conditions
40% of the result from WEKA was used as the training dataset.
The voxel accuracy of the validation set is around 96%.
Three-phase contact points for the water-wet carbonate appear more realistic using GGIECN

## Slide 16
Water-wet reservoir carbonate
Image
GGIECN
WEKA
Verify the applicability of the workflow under complex structural conditions
40% of the result from WEKA was used as the training dataset.
The voxel accuracy of the validation set is around 96%.
GGIECN filtered out fluctuations due to the low resolution of the data

## Slide 17
Water-wet & mixed wet reservoir carbonate
Even though only 40% of the data was used for training, the distribution of contact angles for the workflow is generally consistent with Alhammadi (2017)
Alhammadi, A. M., AlRatrout, A., Singh, K., Bijeljic, B., & Blunt, M. J. (2017). In situ characterization of mixed-wettability in a reservoir rock at subsurface conditions. Scientific Reports, 7 (1), 10753.

## Slide 18
Future work
Combine GGIECN with Jack's super-resolution approach.
Optimisation of computational methods to capture Minkowski functionals.

## Slide 19
Future work
Porous media 3D-SAM (Segment Anything)
Generalised mega-model trained on large amounts of data